4 The Gables N10 3EA


Date of survey 30/05/2023

Rear bedroom windows

The existing windows are softwood and glazed with 3mm clear float 
They are original to the property
There has been an historical leak of the guttering to the left hand side of the double window
which has now been rectified but has caused water ingress to damage the internal plaster wall and sections of the window itself 
although these have now been filled and painted. The sills have been cut back along the front at some point which means that they are not bridging
the concrete sills. There is a mastic seal along the front edge to try and weather this but it's already lifting so water can now penetrate between
the concrete sill and the underside of the wooden sill. The windows also have cables running through the sills which again can cause water ingress over time.
The pulley stiles have also collapsed at pocket level and the pointing is coming away between the vertical reveals and the windows themselves.
The windows are loose fitting, rattling and drafty and in my view have now reached the point of being beyond repair
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